## Slide 1: Study and development of new radon adsorbents The IRENE project
Krakow 3 october 2024
José Busto
CPPM / Univ. Aix-Marseille

## Slide 2
Innovative mateRials for Extreme radoN capturE
4-year funding project (ANR)
5 labs consortium
Particle physicist + Chemist and Physico-chemist
Experimentalist + theoreticians
IRENE

## Slide 3
Natural, Radioactive, Noble gas
from the U and Th chains
Easy to transport, complicated to capture
Short half-life, high intrinsic activity

## Slide 4
Rn Noble gas
Radon Capture
--> no chemistry => physical process : physical adsorption
--> porous materials
Physical adsorption : Surface capture by Van der Waals forces
But not all pores are equally effective
Need to optimise porosity

## Slide 5
Porosity
Activated Charcoal : universal adsorbent (very big surface area (2000 m2/g),
big stability, not toxic, low cost , …)
Activated charcoal : very popular for radon capture
: dozens of papers are published

## Slide 6
2015 : Capture of Rn in over 60 commercial or research materials by dynamic adsorption (SuperNEMO)
- Activated charcoals
- Carbon molecular sieves
- Carbon aerogels (Granada)
- Molecular cages - CC3 (Liverpool)
- MOF
Zeolites (Al, Si) (Marseille, Mulhouse)
Dedritic polymers (Marseille )
Motivation of the IRENE projet
Pressure = 1 bar
Temperature = +20°C à – 80°C
Gas : N2, He
Rn retention time in the column
Rn reduction factor of the column
Adsorption factor

## Slide 7
Chart: Correlation Factor Adsoption v.s. porosite
| 0 | V<0.5 nm | V0.5-0.7 nm | V0.7-0.9 nm | V0.9-1.2 nm | V1.2-1.6 nm | V1.6-2 nm | V<2 nm
K +20 C | 0 | 0.52071 | 0.63441 | 0.62329 | -0.65135 | -0.4839 | -0.48051 | -0.32304
K 0 C | 0 | 0.14103 | 0.59143 | 0.042759 | -0.33842 | -0.50215 | -0.30707 | -0.11592
K-30 C | 0 | 0.4085 | 0.49058 | 0.011248 | -0.28666 | -0.45601 | -0.29274 | -0.18133
K-50 C | 0 | 0.10848 | 0.6918 | 0.16748 | -0.62133 | -0.5599 | -0.56217 | -0.12336
K_0 Arrhen | 0 | 0.61024 | 0.095637 | -0.2612 | 0.095442 | -0.47321 | 0.034297 | -0.43514
- Optimal porosity :
0.5 - 0.7 nm (Rn 0.4 nm)
- Small effect on the chemical
composition (sulphur)
Some results
Adsorption @ – 50°C and -30°C in AC, CMS, Aerogels
AC CMS Aerogel
Microporosity from 0.5 to 2 nm : IJL
Chemical compostion : CINaM
- 30°C
- 50°C

## Slide 8
2018 : Study of Xe / Rn adsorption with Crytophane supramolecular cages
Motivation of the IRENE projet
Very efficient for molecular encapsulation .
Already used for Xe capture
Adjustable cage dimensions
Three cages were studied on two different supports
Silica MCM-41
diamètre de 2,6 nm 6,5 nm.
Silica SBA-14
1000 m2/g
500 m2/g
cages
supports

## Slide 9
Rn adsorption in N2 (CPPM)
Xe adsorption (MADIREL)
Activated charcoal Silcarbon K48 180 ± 25
Rn(K48)/Xe(YC125) « selectivity » = 7.8
Very preliminary results.
- Possibility of improving the performance
(type and size of cage, chemical composition, support).
1,68
13.12

## Slide 10
2020 : Study of radon capture on commercial silver zeolites by dynamical adsorption
Motivation of the IRENE projet

## Slide 11
Adsorption on silver zeolites
(2020 -2023)
- Closed circuit: very high adsorption (very long measurement time)
Breakthrough curbe @-30°C in
0.2 g ETS-10-Ag, 60 l/h N2

## Slide 12
Some results
[m3/kg]
Active Charcoal
Ag Zeolite
1 Reference charcoal (CarboAct®)
3 Commercial Ag zeolites
Ag-ZSM-5
Ag-13X
Ag-ETS-10

## Slide 13
Some results
[m3/kg]
Active Charcoal
Ag Zeolite
1 Reference charcoal (CarboAct®)
3 Commercial Ag zeolites
Ag-ZSM-5
Ag-13X
Ag-ETS-10
~ 100

## Slide 14
[m3/kg]
Active Charcoal
Ag Zeolite
Zeolite NO Ag
1 Reference charcoal (CarboAct®)
3 Commertial Ag zeolites
Ag-ZSM-5
Ag-13X
Ag-ETS-10
2 NO Ag zeolite
13X
ETS-10
Some results
Huge impact of silver on adsorption

## Slide 15
High concentration of 226Ra
=> high emanation
Some results
High sensibility to the water
=> Very dry gas
Evolution of the g line at 609 keV of 214Bi in AC and ETS-10
with a flow of dry air + Rn
Rn reach equilibrium
Rn is empty by water

## Slide 16
Potential improvement
Cu and Ni seem to be better candidates than Ag, and are less expensive !

## Slide 17
The IRENE project
Project submitted to the ANR in 2022
Project start in February 2024
-Feedback between the 5 laboratories
-Modelling as a guide
-Three families of adsorbents (Zeolites, Cages, Carbon-based) -Xenon as a reference gas -Radon capture in N2, He, and Xe
Project philosophy

## Slide 18
XRD, SEM/EDX analysis of ETS-10 and ZSM-5 zeolites
The samples used (ETS-10, ZSM-5) could be improved by eliminating non-adsorbent phases (quartz, alumina, etc.).
The contribution of silver to the capture of radon needs to be better understood (Ag+, nanoparticles )
Some preliminary results from simulation
Monte Carlo simulation of adsorption of Rn & Xe in zeolites
Simulated Rn adsorption isotherms @ 298K & isosteric heats of adsorption

## Slide 19
Some preliminary results from simulation
How chemical composition of zeolite influences Rn & Xe adsorption

## Slide 20
Conclusion
Low-energy and low-counting rate experiments require materials with extreme purity and ultra-low radon
concentration.
Traditionally, activated carbons has been used to capture radon with a good efficiency. However the
purification levels reached are not always sufficient.
Materials with adsorption capacities more than 100 times higher than the best active carbons are now
commercially available but they do not have the necessary purity levels and their performance are not well
understood.
-Possible improvements in radon capture can be reached by choosing the right chemical composition and
good porous structure.
-The objective of the IRENE project is to tackle the problem of radon capture in microporous materials
in a scientific and coherent way, thanks to a unique consortium of physical chemists and particle physicists

## Slide 21
IRENE
Thank you for your attention