## Slide 1
Reducing Background in Germanium Detectors
Early Developments, Recent Applications
Some Issues for CUPID
Frank Avignone
University of South Carolina
Columbia, South Carolina, USA
Some early History in Neutrino Physics; Cerca 1960s
1

## Slide 2
2

## Slide 3
3

## Slide 4
4

## Slide 5
The Beginning of my story was reading the article by Ettore Fiorini et al., “A search for lepton non-conservation in double beta decay with a germanium detector.” Physics Letters B 25 (1967) 602
This started a long series of experiments finally ending with isotopic enrichment with: GERDA, MAJORANA and LEGEND-200 and the projected future LEGEND-1000.
The Mont Blanc Tunnel Experiment
April 1933 to April 2023
5

## Slide 6
6

## Slide 7
A
B
C
D
E
A. Ordinary Cryostat Assembly and 10 cm of lead
B. New Cryostat, Selected Materials, Anti-cosmic Shield, Above Ground
C. 4000 Meter Water Equivalent Overburden, Modern Lead & Copper
Inner Shield
D. Replace Copper Shield With 10 cm of 448 Year old Spanish Galleon
Ballast Lead
E. Replace a Lead Solder Connection with a Crimp Connector.
PNL-USC 1980 - 1983
7

## Slide 8
Let’s Try Electroforming a Copper Cryostat!
8

## Slide 9
Looks Promising!
9

## Slide 10
Cerca 1983, Jim Reeves’ Garage
10

## Slide 11
This Was Our First Attempt Made in the Early 1980s For the First Dark=Matter Search
11

## Slide 12
12

## Slide 13
13

## Slide 14
The First Attempt at an IGEX Cryostat.
14

## Slide 15
Pacific Northwest-Univ. South Carolina
~1988
The International Germanium
Experiment “IGEX” Format.. Two 100% Efficient Ge Detectors in Electroformed Copper Cryostats.
15

## Slide 16
Pacific Northwest-Univ. South Carolina
~1988
The International Germanium
Experiment “IGEX” Format.. Two 100% Efficient Ge Detectors in Electroformed Copper Cryostats.
16

## Slide 17
17

## Slide 18
18

## Slide 19
The MAJORANA DEMONSTRATOR Collaboration via PNNL Grows Major Copper Parts
19

## Slide 20
In MAJORANA, Even Large Pieces of Inner Shielding Were of Electroformed Copper!
20

## Slide 21
21

## Slide 22
50 KW RF
22

## Slide 23
The MELLEN Sunfire Furnace
Purchased be the University of South Carolina with NSF Funding.
It is about 7 ft between Flanges.
It Runs by Heating Coils that are Programmed to Move Heat Zones at Selected Speeds over the Sample.
It needs 80 Amps of 240 V
Single Phase power.
For Pure N2 Gas, One Uses Gas from a LN-Tank
That lasts for more than 30 d.
23

## Slide 24
This is a Perfectly Safe Device!
Any Undergraduate or Graduate Student can Master its Operation in a very Brief Time.
The Contacts Shown are Low-Voltage Thermistor Wires.
Touching The Main Body During Operation is safe.
Very minor Burns Can Occur by Touching the End Flanges During Operation.
24

## Slide 25
For Hydrogen we use a Parker-Hannaford 100 cc/min generator.
The price is < 10 K$
It eats only Deionized Water.
25

## Slide 26
A 1.16 kg bar of Zone-refined Ge ready to be M Measured for Resistivity
26

## Slide 27
50 KW RF
27

## Slide 28
A Jandel Four-Probe Resistivity Measurement set-up.
What about temperature control?
28

## Slide 29
The Industrial standard is to have a temperature-controlled room to keep everything at 20C.
This is costly and unnecessary!
Instead, just use High-quality Laser Thermometer. Then make the small corrections given in the Table on the next view.
29

## Slide 30
29

## Slide 31
30

## Slide 32
The SUNFIRE could be placed underground, or near an underground space, with some overburden to reduce cosmic-ray activation of the Ge.
The plot shows spectra from (red) Ge detectors made from Ge that remained underground whenever not in production. The 3H-beta spectrum is significantly Reduced.
Figure taken from the MAJORANA
Publication-NIM, A 877,314 (2018)
Tritium Production in Ge by Cosmic-Ray Neutrons; How to Minimize it.
31

## Slide 33
32

## Slide 34
33

## Slide 35
34

## Slide 36
35

## Slide 37
How about purification of the initial materials for the Li2MoO4 for CUPID?
36

## Slide 38
37

## Slide 39
38

## Slide 40
39

## Slide 41
After several zonings we loose stoichiometry and form another Li Compound ???
40

## Slide 42
Our TeO2 crystals for CUORE were grown with the Bridgman growth technique, but with seed crystals to grow single crystals.
Growing single crystals maintains stoichiometry and the CUORE crystals did show evidence of good stoichiometry.
Bridgeman single crystal growth requires a large single crystal as a seed. This is not practical with isotopically enriched MoO3; The seeds must be grown by the Czochralski method that requires only a tiny seed.
A small CUORE team tested using a natural abundance TeO2 seed for a Bridgman crystal growth with enriched TeO2. The total crystal suffered significant isotopic dilution.
41

## Slide 43
CONCLUSION
Many of the LEGEND-1000 Ge-Detector Blanks will likely be grown in the Oak Ridge, Tennessee region. Therefore, reprocessing of scrap should be done nearby.
Using new developments built on our experience from the MAJORANA DEMONSTRATOR Project, it may be wise to consider alternative approaches developed since.
A MELLEN SUNFIRE could be located in a university laboratory or in a small building, and operated by students trained in the techniques including the careful preservation of valuable isotopically enriched Ge.
For CUPID, zone-refining and re-zone-refining can cause the loss of Stoichiometry.
For high level of purification, a single-crystal growth method will probably be required; Czochralsky for large seeds, or for the purification growth itself.
42